PROJECT TITAN

Material Trade Study

Educational Engineering Project

| Document Number | TITAN-MAT-001 |
| --- | --- |
| Revision | A |
| Status | Released - Educational Baseline |
| Author | Michael Lozada-Longog |
| Affiliation | Biomedical Engineering, Hawaii Pacific University |
| Date | July 2026 |
| Classification | Educational Engineering Project |

IMPORTANT SCOPE NOTICE

Project TITAN is an educational design and analysis project. It is not a clinically validated device, regulatory submission, or product cleared for human use.

# Document Control and Revision History

| Revision | Date | Description | Prepared By | Status |
| --- | --- | --- | --- | --- |
| A | July 2026 | Initial material screening and weighted selection for baseline structural components. | Michael Lozada-Longog | Released |

Source baseline: Project TITAN Engineering Design Report (July 2026), CAD assembly, completed engineering drawings, and Fusion 360 static FEA results documented by the author.

# 1. Purpose

This trade study compares candidate materials for Project TITAN structural plates and frame members. The goal is not to identify a universally superior material, but to select the most appropriate baseline material for an educational, low-volume, CNC-oriented mechanical prototype.

# 2. Candidate Materials

6061-T6 aluminum

7075-T6 aluminum

316L stainless steel

Ti-6Al-4V titanium alloy

Carbon-fiber-reinforced polymer (CFRP) concept

PEEK engineering polymer

# 3. Selection Criteria and Weighting

| Criterion | Weight | Reason |
| --- | --- | --- |
| Specific strength / mass efficiency | 25% | Wearable-oriented concepts benefit from reduced mass while preserving strength. |
| Machinability and prototype simplicity | 20% | Current development strategy relies on conventional CNC milling and turning. |
| Cost and availability | 20% | Educational prototyping requires readily available stock and manageable replacement cost. |
| Corrosion/environmental resistance | 15% | The concept may be exposed to humidity and handling; future wearable use could introduce sweat. |
| Stiffness and dimensional stability | 10% | Alignment of the shaft and bearings depends on structural stiffness. |
| Documentation and supply familiarity | 10% | Well-characterized, standardized materials simplify analysis and sourcing. |

Scoring scale: 1 = poor, 2 = below average, 3 = acceptable, 4 = good, 5 = excellent. Scores represent an educational engineering judgment for this project scope, not certified supplier ratings.

# 4. Qualitative Property Comparison

| Material | Relative Density | Relative Strength | Machinability | Corrosion Resistance | Prototype Cost | Key Tradeoff |
| --- | --- | --- | --- | --- | --- | --- |
| 6061-T6 Al | Low | Moderate | Excellent | Good | Low | Balanced baseline; lower strength than 7075 or titanium |
| 7075-T6 Al | Low | High | Good | Moderate | Moderate | Higher strength, but costlier and less corrosion/weld friendly |
| 316L Stainless | High | Moderate | Fair | Excellent | Moderate | Excellent corrosion resistance with substantial mass penalty |
| Ti-6Al-4V | Medium | Very high | Difficult | Excellent | Very high | Exceptional performance but expensive and difficult to machine |
| CFRP concept | Very low | Direction-dependent high | Specialized | Excellent | High | Anisotropy, joining, edge damage, and inspection complexity |
| PEEK | Low | Low to moderate | Good | Excellent | High | Light and chemically resistant but low stiffness for baseline structure |

# 5. Weighted Decision Matrix

| Material | Specific strength | Machinability | Cost/availability | Corrosion resistance | Stiffness | Supply familiarity | Weighted Score |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 6061-T6 Al | 4 | 5 | 5 | 4 | 3 | 5 | 4.40/5 |
| 7075-T6 Al | 5 | 4 | 3 | 3 | 3 | 4 | 3.80/5 |
| 316L Stainless | 2 | 2 | 3 | 5 | 5 | 5 | 3.25/5 |
| Ti-6Al-4V | 5 | 1 | 1 | 5 | 4 | 3 | 3.10/5 |
| CFRP concept | 5 | 1 | 1 | 5 | 4 | 2 | 3.00/5 |
| PEEK | 2 | 4 | 2 | 5 | 1 | 3 | 2.85/5 |

# 6. Selection Rationale: 6061-T6 Aluminum

## 6.1 Strength-to-Weight Balance

6061-T6 provides a practical combination of low density, moderate yield strength, and sufficient stiffness for the current load case. The refined assembly FEA met the project safety-factor target with a reported minimum safety factor of 2.377 under the documented idealized setup. Therefore, the baseline does not presently require the cost and manufacturing burden of a higher-performance alloy solely to satisfy the educational static requirement.

## 6.2 Manufacturability

The geometry is dominated by plates, bores, slots, spacers, and a cylindrical shaft. These features align well with CNC milling, drilling, and turning in 6061-T6. The alloy is familiar to machine shops, commonly stocked, and suitable for iterative prototype changes.

## 6.3 Environmental Suitability

Aluminum develops a passive oxide layer and can be anodized for improved surface durability. This makes 6061-T6 preferable to unprotected carbon steel for humid handling environments. This statement does not establish sweat, cleaning-agent, or biocompatibility performance; those conditions require separate verification.

## 6.4 Cost and Educational Value

6061-T6 allows the design to be fabricated and, if desired, destructively tested without the high material and machining costs associated with titanium or composite construction. It is therefore a strong baseline for learning, iteration, and physical validation.

# 7. Part-Specific Material Recommendations

| Component | Baseline | Future Candidate | Reason for Future Review |
| --- | --- | --- | --- |
| Side plates | 6061-T6 aluminum | 7075-T6 or topology-optimized 6061 | Potential mass reduction or higher fatigue margin |
| Upper/lower frames | 6061-T6 aluminum | 6061-T6 retained or CFRP hybrid | Mass and ergonomic improvement |
| Spacers | 6061-T6 aluminum | Acetal/PEEK depending interface | Friction, wear, isolation, and mass |
| Main shaft | 6061-T6 in current drawings | 17-4PH stainless or hardened alloy steel | Bearing wear, surface hardness, bending, and durability |
| Bearings | 52100 bearing steel concept | Sealed corrosion-resistant COTS bearing | Contamination and wearable-environment durability |

Important Design Note The current drawing package identifies the main shaft as 6061-T6 aluminum. For a physical, cyclic, or wearable prototype, the shaft material must be revisited because bearing contact, wear resistance, surface hardness, and repeated bending may make a steel shaft preferable.

# 8. Sensitivity and Decision Risks

If measured loads exceed the current static assumptions, the material ranking may shift toward 7075-T6 or titanium.

If corrosion and cleaning compatibility dominate, 316L stainless may become more attractive despite its mass.

If mass becomes the dominant requirement, CFRP may rank higher but would require a new joint, inspection, and manufacturing architecture.

If direct skin contact or sterilization is introduced, material selection must include biocompatibility and cleaning requirements not evaluated here.

# 9. Decision

Selected Baseline Material 6061-T6 aluminum remains the selected baseline for the side plates, frames, and spacers because it achieved the highest weighted score for this educational prototype. The selection is conditional on the current static load case, machining-oriented build plan, and non-clinical scope.

# 10. Verification Actions

| Action | Purpose | Status |
| --- | --- | --- |
| Confirm CAD material assignments | Ensure mass and FEA use intended baseline properties | Completed for analysis baseline |
| Obtain stock certifications before fabrication | Confirm actual alloy and temper | Future |
| Inspect dimensions and finish | Confirm manufactured parts meet drawings | Future |
| Conduct static and cyclic testing | Compare physical response with analysis | Future |
| Reassess shaft material | Address wear and bearing-interface durability | Required before physical V2 |

# References

Project TITAN Engineering Design Report, July 2026.

Kaiser Aluminum, flat-rolled aluminum product information for 6061 and 7075 alloys.

TIMET, TIMETAL 6-4 technical data sheet.

Typical candidate-property ranges are used for conceptual comparison; procurement must use supplier-certified values.